SECTION 09900

CONCRETE EXTERIOR

SERIES 156 EVIROCRETE

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Coatings systems for exterior concrete.

1.2	RELATED SECTIONS

A.	Section 15075 – Mechanical Identification: Identification of mechanical equipment.

B.	Section 16075 – Electrical Identification: Identification of electrical equipment.

1.4	DEFINITIONS

A.	Definitions of Painting Terms:  ASTM D 16, unless otherwise specified.

B.	Dry Film Thickness (DFT):  Thickness of a coat of paint in fully cured state measured in mils (1/1000 inch).

1.5	SUBMITTALS

A.	Comply with Section 01330 - Submittal Procedures.

B.	Product Data:  Submit manufacturer's product data for each coating, including generic description, complete technical data, surface preparation, and application instructions.

C.	Color Samples:  Submit manufacturer’s color samples showing full range of standard colors.

D.	Manufacturer’s Quality Assurance:  Submit manufacturer’s certification that coatings comply with specified requirements and are suitable for intended application.

E.	Applicator’s Quality Assurance:  Submit list of a minimum of 5 completed projects of similar size and complexity to this Work.  Include for each project:

1.	Project name and location.

2.	Name of owner.

3.	Name of contractor.

4.	Name of engineer.

5.	Name of coating manufacturer.

6.	Approximate area of coatings applied.

7.	Date of completion.

F.	Warranty:  Submit manufacturer’s standard warranty.

G.	Include as part of the bid requirements:

1. Outline of expected procedures to perform the scope of work for the cities review.

2. Time line

1.6	QUALITY ASSURANCE

A.	Manufacturer’s Qualifications:

1.	Specialize in manufacture of coatings with a minimum of 10 years successful experience.

2.	Able to demonstrate successful performance on comparable projects.

3.	Single Source Responsibility:  Coatings and coating application accessories shall be products of a single manufacturer.

B.	Applicator’s Qualifications:

1.	Experienced in application of specified coatings for a minimum of 5 years on projects of similar size and complexity to this Work.

2.	Applicator's Personnel:  Employ persons trained for application of specified coatings.

C.	Pre-application Meeting:  Convene a pre-application meeting on the first day of production before start of application of coating systems.  Require attendance of parties directly affecting work of this section, including Contractor, Engineer, applicator, and manufacturer’s representative.  Review the following:

1.	Environmental requirements.

2.	Protection of surfaces not scheduled to be coated.

3.	Surface preparation.

4.	Application.

5.	Repair.

6.	Field quality control.

7.	Cleaning.

8.	Protection of coating systems.

9.	One-year inspection.

10.	Coordination with other work.

1.7	DELIVERY, STORAGE, AND HANDLING

A.	Delivery:  Deliver materials to site in manufacturer's original, unopened containers and packaging, with labels clearly identifying:

1.	Coating or material name.

2.	Manufacturer.

3.	Color name and number.

4.	Batch or lot number.

5.	Date of manufacture.

6.	Mixing and thinning instructions.

B.	Storage:

1.	Store materials in a clean dry area and within temperature range in accordance with manufacturer's instructions.

2.	Keep containers sealed until ready for use.

3.	Do not use materials beyond manufacturer’s shelf life limits.

C.	Handling:  Protect materials during handling and application to prevent damage or contamination.

1.8	ENVIRONMENTAL REQUIREMENTS

A.	Weather:

1.	Air and Surface Temperatures:  Prepare surfaces and apply and cure coatings within air and surface temperature range in accordance with manufacturer’s instructions.

2.	Surface Temperature:  Minimum of 5 degrees F (3 degrees C) above dew point.

3.	Relative Humidity:  Prepare surfaces and apply and cure coatings within relative humidity range in accordance with manufacturer’s instructions.

4.	Precipitation:  Do not prepare surfaces or apply coatings in rain, snow, fog, or mist.

5.	Wind:  Do not spray coatings if wind velocity is above manufacturer’s limit.

PART 2	PRODUCTS

2.1	MANUFACTURER

Tnemec Company, Inc., is listed as the standard of excellence.  Substitutions shall be considered but must be approved by Engineer prior to bid deadline. Offers for substitutions will not be considered which decrease film thickness, solids by volume or the number of coats to be applied or which propose a change from the generic type of coating specified herein. All substitutions shall include complete test reports to comply with specified performance criteria. Paint application shall be in strict accordance with manufacturer's printed instructions except that coating thickness specified in paint schedule herein shall govern.

2.2	COATING SYSTEMS PERFORMANCE

Exterior Coatings

A. ASTM D 4585 Humidity:

System: One coat Series 156 Enviro-Crete applied directly to concrete and cured 7 to 10 	days at 75°F (24°C) and 50% R.H.

Requirement: No blistering, cracking or visible damage after 2,000 hours exposure.

B. ASTM D 1653 (Water Vapor Transmission):

No more than 37.44 g/m2 per 24h water vapor transmission (WVT), and no more than 3.09 perms (2.03 metric perms) water vapor permeance (WVP).

C. ASTM D 4587 QUV:

No blistering, cracking, chalking or delamination of the film. No less than 69% gloss   retention, no more than 1.1 units gloss loss, and no more than 3.59 DE (FMC-2) after  5,000 hours QUV exposure

D. ASTM B117 Salt Fog:

No blistering, cracking or delamination of film. No visible damage to coating or substrate  after 5,000 hours.

2.4	COATINGS SYSTEMS FOR EXTERIOR OF CONCRETE

(Generic Desciption – Waterborne Acrylate)

A. 	Optional Primer (Consult Tnemec):  Tnemec Series 151 Elasto-Grip FC at 1.0-2.0 mils DFT

B.	Prime Coat: Tnemec Series 156 EnviroCrete applied at 6 to 8 mils DFT.

B.	Full Coat: Tnemec Series 156 EnviroCrete applied at 6 to 8 mils DFT.

2.5	ACCESSORIES

A.	Coating Application Accessories:

1.	Accessories required for application of specified coatings in accordance with manufacturer’s instructions, including thinners.

2.	Products of coating manufacturer.

PART 3	EXECUTION

3.1	EXAMINATION

A.	Examine areas and conditions under which coating systems are to be applied.  Notify Engineer of areas or conditions not acceptable.  Do not begin surface preparation or application until unacceptable areas or conditions have been corrected.

3.2	PROTECTION OF SURFACES NOT SCHEDULED TO BE COATED

A.	Protect surrounding areas and surfaces not scheduled to be coated from damage during surface preparation and application of coatings.

B.	Immediately remove coatings that fall on surrounding areas and surfaces not scheduled to be coated.

3.3	SURFACE PREPARATION OF CONCRETE

A.	Prepare concrete surfaces in accordance with manufacturer’s instructions and per SSPC-SP13/NACE 6.

3.4 	SURFACE PREPARATION

A.     Exterior Concrete Surfaces:

All exterior existing coated surfaces shall receive at minimum, high-pressure wash – 1,500 PSI at 3.5 gallons per minute minimum. Surface is to be clean, dry and free of contaminants.

3.6	APPLICATION

A.	Apply coatings in accordance with manufacturer's instructions, including crack treatment if necessary.

B.	Mix and thin coatings, including multi-component materials, in accordance with manufacturer’s instructions.

C.	Keep containers closed when not in use to avoid contamination.

D.	Do not use mixed coatings beyond pot life limits.

E.	Use application equipment, tools, pressure settings, and techniques in accordance with manufacturer’s instructions.

F.	Uniformly apply coatings at spreading rate required to achieve specified DFT.

G.	Apply coatings to be free of film characteristics or defects that would adversely affect performance or appearance of coating systems.

3.8	REPAIR

A.	Damaged Materials:  Repair or replace damaged materials and surfaces not scheduled to be coated.

B.	Damaged Coatings:  Touch-up or repair damaged coatings.  Touch-up of minor damage shall be acceptable where result is not visibly different from adjacent surfaces.  Recoat entire surface where touch-up result is visibly different, either in sheen, texture, or color.

C.	Coating Defects:  Repair in accordance with manufacturer’s instructions coatings that exhibit film characteristics or defects that would adversely affect performance or appearance of coating systems.

3.9	FIELD QUALITY CONTROL

A.	Inspector’s Services:

1.	Verify coatings and other materials are as specified.

2.	Verify surface preparation and application are as specified.

3.	Verify DFT of each coat and total DFT of each coating system are as specified using wet film.

4.	Coating Defects:  Check coatings for film characteristics or defects that would adversely affect performance or appearance of coating systems.

5.	Report:

a.	Submit written reports describing inspections made and actions taken to correct nonconforming work.

b.	Report nonconforming work not corrected.

c.	Submit copies of report to Engineer and Contractor.

B.	Manufacturer’s Field Services:  Manufacturer’s representative shall provide technical assistance and guidance for surface preparation and application of coating systems.

3.10	CLEANING

A.	Remove temporary coverings and protection of surrounding areas and surfaces.

3.11	PROTECTION OF COATING SYSTEMS

A.	Protect surfaces of coating systems from damage during construction.

3.12	ONE-YEAR INSPECTION

A.	Owner will set date for one-year inspection of coating systems.

B.	Inspection shall be attended by Owner, Contractor, Engineer, and manufacturer’s representative.

C.	Repair deficiencies in coating systems as determined by Engineer in accordance with manufacturers instructions.

END OF SECTION